Supporting Information

Sub-micron patterning of metal oxide surfaces via microcontact printing and microtransfer molding of amphiphilic molecules and antifouling application

Josué Cordero Guerrero1, Gabriel Jiménez Thuel1 and Sergio A. Paniagua*2,3 ORCID ID

1Chemistry Graduate Program, Universidad de Costa Rica, San José, Costa Rica

2Natural Sciences Department, Universidad de Costa Rica, Alajuela, Costa Rica
3National Nanotechnology Laboratory (LANOTEC), CENAT-CONARE, San José, Costa Rica.

*Address all correspondence to this author: spaniagua@cenat.ac.cr / sergio.paniagua@ucr.ac.cr

Fig. S1. AFM of DVD-R (a) and a PDMS replica (b) with their corresponding cross sections across at mid image.

Fig. S2. AFM of CD-R (a) and a PDMS replica (b) with their corresponding cross sections at mid image.

Table S1. Summary of observations for smooth clean substrates, monolayer-coated smooth controls and patterned samples.

| Sample | Film / Pattern Thickness (nm) | Crest FWHM (nm) | Observed water contact angle (°) |
| --- | --- | --- | --- |
| Freshly cleaned mica | NA | NA | Complete wetting (<30°) |
| Spread coated ODPA on mica* | 1.4±0.2 | NA | 78±10 |
| µCP (DVD-R) ODPA on mica | 6.7±0.3 | 430±80 | 43±5 |
| Plasma cleaned Si wafer | NA | NA | Complete wetting (<30°) |
| Spread coated ODPA on Si wafer | NA | NA | 92±1 |
| µCP ODPA (DVD-R) on Si water | 1.9±0.4 | 390±60 | 93±5 |
| Electropolished Al AA6063 (EP Al) plasma cleaned | NA | NA | 32±3 |
| Monolayer ODPA on EP Al | NA | NA | 95±5 |
| µTM ODPA (CD-R) on EP Al | 850±80 | 150±20 | 110±1 |
| µTM ODPA (CD-R) on EP Al/Etchant A/ML ODPA | 820±80 | 150±30 | 110±4 |
| µTM OTES (DVD-R) on EP Al | 420±40 | 55±6 | 101±3 |
| µTM OTES (DVD-R) on EP Al/Phosphoric acid etch | 310±50 | 46±2 | 31±6 |
| µTM OTES (DVD-R) on EP Al/Acid etch/Plasma strip | 300±30 | 33±3 | Complete wetting (<30°) |

*AFM shown in Fig. S3.

Fig. S3. AFM of spread-coated ODPA on mica (left) and cross section view of heights following white line (left).